API SPEC 5L/ 5CT
	Product name
	Executive standard
	Dimension (mm)
	Steel code/ Steel grade

	Casting
	API 5CT
	114-219 x 5.2-22.2
	J55, K55, N80, L80, P110

	Tubing
	API 5CT
	48.3-114.3 x 3.2-16
	J55, K55, N80, L80, H40

	Casting
	API 5L
	10.3-1200 x1.0-120
	A, B, X42, X46, X52, PSL1 / PSL2

	Drill Pipe
	API 5DP
	Outer diameter: 2 3/8'-51/2'
Wall thickness: 6.45mm-12.7mm
Length: R1,R2 and R3
	E75, X95, G105, S135 .


ASTM / ASME
	Product name
	Executive standard
	Dimension (mm)
	Steel code/ Steel grade

	Black and Hot-dipped Zinc-coated Steel Pipes Seamless
	ASTM A53
	0.3-1200 x 1.0-150
	GR.A, GR.B, GR.C

	Seamless Carbon Steel for High Temperature Service
	ASTM A106
	10.3-1200 x 1.0-150
	GR.B, GR.C

	Seamless Cold-drawn Low-Carbon Steel Heat-Exchanger and Condenser Tubes
	ASTM A179
	10.3-426 x 1.0-36
	Low Carbon Steel

	Seamless Carbon Steel Boiler Tubes for High Pressure
	ASTM A192
	10.3-426 x 1.0-36
	Low Carbon Steel

	Seamless Cold-drawn Intermediate Alloy Steel Heat-exchanger and Condenser Tubes
	ASTM A199
	10.3-426 x 1.0-36
	T5, T22

	Seamless Medium-carbon Steel Boiler and Superheater Tubes
	ASTM A210
	10.3-426 x 1.0-36
	A1, C

	Seamless Ferritic and Austenitic Alloy Steel Boiler, Superheater and Heat-exchanger Tubes
	ASTM A213
	10.3-426 x 1.0-36
	T5, T5b, T9 , T11, T22 ,T91

	Seamless Carbon and Alloy Steel for Mechanical Tubing
	ASTM A333
	1/4"-42" x SCH20-XXS
	Grade1 Gr. 3,Gr..6, Gr.8 , Gr. 9

	Seamless Cold-drawn Carbon Steel Feedwater Heater Tubes
	ASTM A556
	10.3-426 x 1.0-36
	A2, B2

	For seamless ferritic alloy-steel pipe for high-temperature service
	ASTM A335
	1/4"-42" x SCH20-XXS
	A/SA 335 P1, P2, P11, P12, P15, P22, P91, P92, P122


DIN/EN
	Product name
	Executive standard
	Dimension (mm)
	Steel code/ Steel grade

	Seamless Steel Tubes for Elevated Temperature
	DIN 17175
	10-762 x 1.0-120
	St35.8,St45.8, 10CrMo910, 15Mo3, 13CrMo44, STPL340, STB410, STB510, WB36

	Seamless Circular Tubes of Non Alloys Steels with Special Quality Requirements.
	DIN 1629
	13.5-762 x 1.8-120
	St37.0, St44.0, St52.0

	Seamless steel tubes for pressure purposes
	EN 10216
	4.0-60.0 x 0.5-8
5-7 m manufacturing lenght
	P235GH TC1, P235GH TC2, 16Mo3

	hydraulic and pneumatic power system, low-voltage circuit, power steering, fuel circuit, vibration reduction, and such.
	EN 10305
	13.5-165.1 x 1.8-4.85
	St33.2

	specifies the Seamless steel tubes used forMechanical and Automobile.
	DIN 2391
	4.0-60.0 x 0.5-8
	St35, St45, St52

	Seamless Steel Tubes
	DIN 2440
	13.5-165.1 x 1.8-4.85
	St33.2


JIS
	Product name
	Executive standard
	Dimension (mm)
	Steel code/ Steel grade

	High pressure and high temperature service
	JIS G3454/5/6
	19.05-114.3 x 2.0-14
	JIS G3454(STPG370, STPG410), JIS G3455(STS370, STS410, STS480), JIS G3456(STPT370, STPT410, STPT480)

	Tubes used for machinery, automobiles, bicycles, furniture, appliances and other machine parts.
	JIS G3445
	19.05-114.3 x 2.0-14
	STKM11A, STKM12(A,B,C), STKM13(A,B,C), STKM14(A,B,C).

	Carbon steel/Alloy steel boiler and heat exchanger tubes
	JIS G3461,2
	19.05-114.3 x 2.0-14
	G3461(STB340, STB410, STB510)
G3462(STBA22, STBA23)

	Seamless steel tubes for high pressure gas cylinder
	JIS G3429
	19.05-114.3 x 2.0-14
Length: max 16000mm
	STH11, STH12, STH21, STH22

	Heat resistant alloy steel pipes that are used for high temperature conveying fluid pipes for heaters and boiler tubes.
	JIS G3458
	10.5-660.4 mm
	STPA 12, STPA 20, STPA 22, STPA 23, STPA 24, STPA 25, STPA 26


GB 国标
	Product name
	Executive standard
	Dimension (mm)
	Steel code/ Steel grade

	Used for manufacturing various low and medium pressure boilers.
	GB 3087
	19.05-114.3 x 2.0-14
	10#, 20#

	Low-temperature heat exchanger tubes seamless steel pipe
	GB/T18984
	19.05-351 x 2.0-14
	06Ni3MoDG, 09DG, 09Mn2VDG, 10MnDG, 16MnDG

	GB 8163 steel pipe is a seamless steel pipe for fluid transportation (GB/T8163-2018)
	GB/T 8163
	19.05-351 x 2.0-14
	10#

	High pressure and above pressure steam boiler tubes with high quality carbon structural.
	GB5310
	19.05-114.3 x 2.0-14
	20G, 20MnG, 25MnG, 15MoG, 20MoG, 12CrMoG, 15CrMoG(T12/P12), 12CrMoG, 12Cr2MoWVTiB.
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